

Soldering Wire

Model: NS3005

Specification:

60%SN/40%PB, Flux:2%

OD:0.71mm

New weight: 200g

Melting point: 183℃