| Cat # | Description |
| --- | --- |
| WB-2030 | Cat 6 UTP Solid Core LAN Cable 100m Roll Length Grey |

| Mechanical Characteristics |  |  |
| --- | --- | --- |
| Conductor | Material | Bare Copper |
|  | Size | 22AWG |
|  | Construction | 1/0.58 ± 0.02mm |
| Insulation | Material | HDPE |
|  | Thickness | Min: 0.2mm, Max Avg: 0.248mm |
|  | Diameter | 1.08 ± 0.2mm |
|  | Colours | Blue + White-Blue |
|  |  | Orange + White-Orange |
|  |  | Green + White-Green |
|  |  | Brown + White-Brown |
|  | Elongation | Minimum 300% |
|  | Tensile Strength | Minimum 1.682kg/mm sq |
| Sheath | Material | PVC |
|  | Thickness | Min 0.46mm, Max Avg 0.58mm |
|  | Diameter | 6.4 ± 0.3 mm |
|  | Colour | Grey |
|  | Elongation | Minimum 100% |
|  | Tensile Strength | Minimum 1.407 kg/mm sq |
|  | Aging @ 100ºC for 168 hours | Minimum elongation retention: 58% |
|  |  | Minimum tensile strength retention: 75% |
| Flame Test |  | Meets AS/ACIF S008:2001 |
| Pair Separator |  | Separate “+” moulding |
| Electrical Characteristics |  |  |
| Spark Test |  | 2000 ± 250V AC |
| Dielectric Strength |  | 2500VDC for 3 Seconds |
| Insulation Resistance Test |  | Minimum 150M Ohm/Km |
| Conductor Resistance |  | Maximum 7.91 Ohm/100M @ 20 deg C |
| Resistance Unbalance |  | Maximum 2% |
| 6. Capacitance Unbalance |  | Maximum 330pF/100M |
| Mutual Capacitance |  | Maximum 5600pF/100M |
| Impedance |  | 64kHz 125 Ohm +/- 20% |
|  |  | 1~250MHz 100 Ohm +/- 15% |
| Attenuation & Near End Cross-talk |  |  |
| Frequency | Attenuation | NEXT | Power Sum |
|  | (dB/100 metres @ 20º C max) | (dB) min | (dB) min |
| 1MHz | 0.0 | 66.0 | 64.0 |
| 4MHz | 3.8 | 65.3 | 63.3 |
| 10MHz | 6.0 | 59.3 | 57.3 |
| 16MHz | 7.6 | 56.2 | 54.2 |
| 20MHz | 8.5 | 54.8 | 52.8 |
| 31.25MHz | 10.7 | 51.9 | 49.9 |
| 62.5MHz | 15.5 | 47.4 | 45.4 |
| 100MHz | 19.9 | 44.3 | 42.3 |
| 155MHz | 25.3 | 41.4 | 39.4 |
| 200MHz | 29.2 | 39.8 | 37.8 |
| 250MHz | 33.0 | 38.3 | 36.3 |